## Slide 1
Irradiation study of Ti-6Al-4V and Ti-6Al-4V-1B for FRIB beam dump:
Aida Amroussia, PhD Student
Chemical Engineering and Materials Science
Michigan State University
May 19, 2014

## Slide 2: Outline
Irradiation of samples with high energy heavy ions (NSCL-MSU)(Ca 40 @ 2000 MeV) and low energy heavy ions at CIMAP-France
XRD and TEM observations( in collaboration with CIMAP)
Surface characterization using SEM-EBSD
Nano-indentation tests
Vickers Hardness tests
Insitu-tensile tests

## Slide 3: Irradiation experiments
Facilities | Beam | Energy [MeV] | Range [µm] | Se [keV/nm] | Fluence [ions/cm2] | Max dpa in sample | Date | Number of samples | Type
IRRSUD | 82Kr | 25 | 4.73 | 9.9 | 5.1011-5.1012-2.1014 | 0.6 | Jul-13 | 6 | Foils
IRRSUD | 131Xe | 92 | 8.5 | 19.7 | 2.1011 | 0.001 | Jul-13 | 2 | Foils
IRRSUD | 82Kr | 45 | 6.43 | 13.1 | 5.1011-5.1013 | 0.16 | Jul-13 | 4 | Foils
IRRSUD | 82Kr | 45 | 6.43 | 13.1 | 2.1014 2.5.1015 | 8 | Oct-13 | 6 | Foils
IRRSUD | 36Ar | 36 | 6.8 | 7.5 | 1015 | 1.5 | Dec-13 | 23 | TEM and dogbone
IRRSUD | 129Xe | 92 | 8.5 | 19.7 | If 3 1014 (~10h) | Estimated 1.7 | Planned in June-2014 |  | 
NSCL | 40Ca | 2000 | 800 | 1.5 | 6 1012 | 10-5 | Aug-13 | 1 x Ti64 | Dogbone

## Slide 4: XRD and TEM observations( in collaboration with CIMAP)
M. Toulemonde et al./ NIMB 277 (212) 28-39
No evidence of phase transformation or ion track formation in Ti-6Al-4V
pristine
Xe 92 MeV – 2 1011 ions/cm²
Intensity (u.a.)
2 θ (º)
  Ti-alloys are not sensitive to electronic excitation by swift heavy ions compared to pure Titanium
TEM image of a Ti-6Al-4V foil irradiated with Kr 45 MeV – 5 1013 ions/cm²
N. Velisavljevic, et al., Titanium Alloys at Extreme Pressure Conditions, Titanium Alloys - Towards Achieving Enhanced Properties for Diversified Applications. (2012)
Notes: Frederique ppt

## Slide 5: Characterization of the microstructure and mechanical properties:
Scanning electron microscopy (SEM) as well as electron backscatter diffraction (EBSD) were used to characterize the microstructure of the samples before and after irradiation.
Nano-indentation , Vickers Hardness and in-situ tensile tests were used to investigate the change in the mechanical properties.

## Slide 6: Observations
Deterioration of the quality of the EBSD scan after irradiation.
Ti-6Al-4V-1B Irradiated at CIMAP: Ar@36MeV
T=350 ͦC and a fluence of 1015 Ions/cm and
dpa at the surface of 0.038dpa
IPF map before irradiation IPF map after irradiation
IPF map before irradiation IPF map after irradiation
Ti-6Al-4V Irradiated at NSCL: Ca@2000MeV
T=20 ͦC and a fluence of 6.1012Ions.cm-2 and dpa at the surface of 10-5dpa
Ti-6Al-4V Ti-6Al-4V-1B

## Slide 7: SEM and EBSD characterization of the surface of the samples:
SEM image of the EBSD area before (a) and after (b) irradiation for Ti-6Al-4V
Irradiated at CIMAP: Ar@36MeV
T= 350 OC
Fluence = 1015 ions.cm-2
Dose at the surface= 0.038dpa
No change in the microstructure or the orientation of the grains at the surface.
IPF and local average misorientation maps the grains before and after irradiation of Ti-6Al-4V
IPF and local average misorientation maps the grains before and after irradiation of Ti-6Al-4V-1B

## Slide 8: Local Average misorientation charts Low energy irradiation: Ar36@36MeV Comparison between Ti-6Al-4V and Ti-6Al-4V-1B only alpha phase
Chart: Ti-6Al-4V- HT-HF Fluence = 1015 ions.cm-2 Temperature = 350OC
Chart: Ti-6Al-4V- HT-LF Fluence = 1014 ions.cm-2 Temperature = 350OC
Chart: Ti-6Al-4V-1B- HT-LF Fluence = 1014 ions.cm-2 Temperature = 350OC
Chart: Ti-6Al-4V-1B- HT-HF Fluence = 1015 ions.cm-2 Temperature = 350OC
Ti-6Al-4V Ti-6Al-4V-1B
Unexpected changes in the local average misorientation for Ti-6Al-4V-1B

## Slide 9: Local Average misorientation charts Comparison between high energy and low energy irradiation
Chart: Ti-6Al-4V Ca40 @2000MeV Fluence = 6.1012 ions.cm-2 Temperature = 20OC
Chart: Ti-6Al-4V- LT-LF Ar36@36MeV Fluence = 1014 ions.cm-2 Temperature = 20OC
At high energy irradiation, the local average misorientation are more affected in Ti-6Al-4V

## Slide 10: Mechanical testing: Nano-indentation
In all samples one grip was masque in order to compare irradiated to not irradiated properties in the same sample
Obtain the properties of the materials in depth.
Parameters:
Berkovich tip
Strain rate : 0.05s-1
Poisson ratio=0.33
Distance between indents: 50µm
Chart: dpa for Φ=1e15 ion/cm2 Ar 36 @ 36 MeV
SEM image of nanoindents matrix in Ti-6Al-4V irradiated at T= 20 OC and a fluence of 1015 ions.cm-2
Non irradiated
Al mask
a
a
Irradiated
Notes: For this tip width= 7*depth= 7*2=14microns

## Slide 11: Nano-indentation results
Chart: Test number
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36
irradiated | 130.729 | 134.454 | 140.281 | 136.722 | 139.996 | 134.016 | 140.456 | 140.254 | 144.837 | 141.002 | 139.281 | 131.615 | 94.884 | 139.493 | 139.671 | 136.945 | 137.946 | 134.007 | 135.517 | 131.863 | 131.61 | 136.865 | 137.101 | 140.221 | 135.649 | 140.058 | 142.289 | 141.742 | 132.368 | 137.381 | 139.833 | 134.715 | 136.605 | 134.969 | 135.031 | 140.431
Non irradiated | 139.174 | 199.267 | 170.953 | 143.334 | 138.404 | 190.757 | 168.015 | 176.193 | 172.303 | 162.282 | 170.307 | 157.722 | 135.595 | 168.157 | 174.745 | 185.502 | 194.507 | 165.464 | 182.208 | 187.514 | 194.626 | 165.268 | 186.709 | 189.394 | 194.98 | 173.48 | 154.118 | 163.974 | 181.674 | 205.224 | 157.305 | 187.99 | 184.888 | 186.28 | 137.599 | 169.752
Chart: Test number
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36
irradiated | 4.676 | 4.825 | 4.568 | 4.683 | 5.11 | 4.767 | 4.766 | 4.664 | 5.354 | 4.578 | 4.75 | 4.486 | 2.305 | 4.968 | 4.745 | 4.55 | 4.439 | 4.782 | 4.642 | 4.491 | 4.715 | 4.737 | 4.928 | 4.677 | 4.803 | 4.829 | 4.925 | 5.029 | 4.455 | 4.842 | 4.45 | 4.517 | 4.795 | 4.82 | 4.871 | 4.752
Non irradiated | 0 | 4.676 | 4.825 | 4.568 | 4.683 | 5.11 | 4.767 | 4.766 | 4.664 | 5.354 | 4.578 | 4.75 | 4.486 | 2.305 | 4.968 | 4.745 | 4.55 | 4.439 | 4.782 | 4.642 | 4.491 | 4.715 | 4.737 | 4.928 | 4.677 | 4.803 | 4.829 | 4.925 | 5.029 | 4.455 | 4.842 | 4.45 | 4.517 | 4.795 | 4.82 | 4.871 | 4.752
Ti-6Al-4V
Ar36 @36MeV
T= 20 OC
Fluence = 1015 Ions.cm-2
Dose= 0.038dpa
No change in hardness was observed
Decrease in the elastic modulus after irradiation
Notes: Tahniten

## Slide 12: Vickers Hardness tests:
Chart: Ti-6Al-4V Fluence = 1015 ions.cm-2 Temperature = 20OC
| 50 | 50 | 50 | 50 | 100 | 100 | 100 | 200 | 200 | 200 | 300 | 300 | 300 | 500 | 500 | 500 | 1000 | 1000
Irradiated | 343.9173 | 329.6948 | 361.3281 | 361.3281 | 362.2053 | 342.2361 | 343.7128 | 351.3762 | 343.9173 | 360.2016 | 324.5951 | 335.8705 | 317.6438 | 329.9209 | 331.7981 | 329.9209 | 333.3183 | 329.3278
Non irradiated | 341.8298 | 334.6713 | 354.6473 | 317.2031 | 337.8625 | 337.8625 | 334.6713 | 341.8298 | 348.1501 | 325.7931 | 316.0437 | 320.7696 | 316.5314 | 320.7127 | 319.1691 | 327.758 | 343.4321
No change in hardness
Chart: Ti-6Al-4V Fluence = 1015 ions.cm-2 Temperature = 350OC
| 100 | 100 | 100 | 200 | 200 | 200 | 300 | 300 | 500 | 500 | 1000 | 1000
Irradiated | 311.3741 | 326.6012 | 355.8787 | 326.762 | 330.6812 | 346.024 | 340.0402 | 333.4054 | 314.2985 | 327.7509 | 327.5773 | 319.8698 | 0
Non irradiated | 340.7688 | 309.4668 | 318.5207 | 314.4948 | 340.7932 | 303.7742 | 318.4051 | 320.7054 | 333.6914 | 314.2985 | 316.9218 | 324.1177 | 326.2735
Ar @36 MeV
Chart: Ti-6Al-4V-1B Fluence = 1015 ions.cm-2 Temperature = 20OC
| 50 | 50 | 100 | 100 | 100 | 200 | 200 | 300 | 300 | 300 | 500 | 500 | 500 | 500 | 1000 | 1000 | 1000
Irradiated | 411.1111 | 411.1111 | 462.5 | 419.5011 | 409.6886 | 392.5771 | 390.032 | 370.5707 | 377.3655 | 376.3835 | 375.2349 | 356.3308 | 382.1303 | 383.6885 | 397.7434 | 376.4746 | 374.8686
Non irradiated | 375.4028 | 370.6358 | 383.6885 | 370 | 357.5202 | 341.7298 | 357.5202 | 369.3638 | 370.5336 | 385.0156 | 436.9339 | 380.0953
Chart: Ti-6Al-4V Fluence = 1015 ions.cm-2 Temperature = 20OC
| 50 | 50 | 50 | 50 | 100 | 100 | 100 | 200 | 200 | 200 | 300 | 300 | 300 | 500 | 500 | 500 | 1000 | 1000
Irradiated | 343.9173 | 329.6948 | 361.3281 | 361.3281 | 362.2053 | 342.2361 | 343.7128 | 351.3762 | 343.9173 | 360.2016 | 324.5951 | 335.8705 | 317.6438 | 329.9209 | 331.7981 | 329.9209 | 333.3183 | 329.3278
Non irradiated | 341.8298 | 334.6713 | 354.6473 | 317.2031 | 337.8625 | 337.8625 | 334.6713 | 341.8298 | 348.1501 | 325.7931 | 316.0437 | 320.7696 | 316.5314 | 320.7127 | 319.1691 | 327.758 | 343.4321

## Slide 13: In-situ Tensile tests: Preliminary results
Chart: Ti-6Al-4V RT Tensile test
Ion beam : Ca 40 @2000MeV
T= 20OC
Fluence = 6.1012 ions.cm-2
Max dpa= 10-5 dpa
SEM images of the same area (a) before the tensile test and (b) at 13% strain
a
b
IPF map , {0001} and {10-10} pole figures of the α phase in the same area before irradiation

## Slide 14: Evolution of the microstructure during the test
Microstructure of irradiated Ti-6Al-4V (a) before the tensile test and (b) at 5.27% strain
a
b
Slip lines
Ion beam : Ca 40 @2000MeV
T= 20OC
Fluence = 6.1012 ions.cm-2
Max dpa= 10-5 dpa

## Slide 15: In-situ Tensile tests: Preliminary results
Ion beam : Ar@36MeV
T= 350 OC
Fluence = 1015 ions.cm-2
Max dpa= 1.5 dpa
SEM images of the same area (a) before the tensile test (b) at 18.7 % strain, (c) failure surface
a
b
Chart: Ti-6Al-4V RT Tensile test
c
IPF map , {0001} and {10-10} pole figures of the α phase in the same area before irradiation

## Slide 16
Microstructure of irradiated Ti-6Al-4V (a) at 6.77% strain and (b) at 9.38% strain
Evolution of the microstructure during the test
Slip lines
Slip lines
a
b
Ion beam : Ar@36MeV
T= 350 OC
Fluence = 1015 ions.cm-2
Max dpa= 1.5 dpa

## Slide 17: In-situ Tensile tests: Preliminary results Texture of the tested Ti-6Al-4V
Ion beam : Ca 40 @2000MeV
T= 20OC
Fluence = 6.1012 ions.cm-2
Max dpa= 10-5 dpa
Ion beam : Ar@36MeV
T= 350 OC
Fluence = 1015 ions.cm-2
Max dpa= 1.5 dpa
Non-irradiated Ti6Al-4V sample [Li.]
Hongmei L,”ANALYSIS OF THE DEFORMATION BEHAVIOR OF THE HEXAGONAL CLOSE-PACKED ALPHA PHASE IN TITANIUM AND TITANIUM ALLOYS”, PhD disseretation , Michigan State University

## Slide 18: In-situ Tensile tests: Comparison with other Ti64 RT tension Test
For low energy irradiation no change in the mechanical properties ( the damage is only on the surface (7 microns).
For high energy irradiation, even at low doses, we observed a significant decrease in the UTS.
More tests are required

## Slide 19: Conclusion
Ongoing analyses:
  Nano-indentation tests on the cross sections of the samples will allow extraction of hardness and Young modulus for different dpa doses.
  In-situ tensile tests: Comparison between non irradiated and irradiated Ti-alloys and slip trace analysis
Future analyses
  New EBSD analyses planned after electro-polishing the samples
  Swelling measurements on each samples
  Possibility to use FIB (Focused Ion Beams) to study the damage in the depth of the sample for TEM, SEM/EBSD analyses
  In-situ irradiation and creep test