## Slide 1: Radiation Damage and Annealing in Graphite: Ways to Improve the Lifetime of Targets
Frederique Pellemoine
Wolfgang Mittig
May 19, 2015

## Slide 2: Outline
FRIB High-power production targets
  Design and challenges
  Irradiation and annealing studies of graphite
    Temperature effect
NSCL-FRIB stripper
  Challenges
  Irradiation and annealing studies of graphite
    Temperature effects
Conclusions

## Slide 3: High-Power Production Target Scope and Technical Requirements
In-flight rare isotope beam production with beam power of 400 kW at 200 MeV/u for 238U and higher energies for lighter ions
High power capability
  Up to 100 kW in a ~ 0.3 - 8 g/cm² target for rare isotope production via projectile fragmentation and fission
Required high resolving power of fragment separator
  1 mm diameter beam spot
  Maximum extension of 50 mm in beam direction
Target lifetime of 2 weeks to meet experimental program requirements
Preseparator
Primary Beam
Production target

## Slide 4: FRIB Production Target Rotating Multi-slice Graphite Target Design
Beam
Rotating multi-slice graphite target chosen for FRIB baseline
  Increased radiating area and reduced total power per slice by using multi-slice target
  Use graphite as high temperature material
  Radiation cooling
Design parameters
  Optimum target thickness is ~ ⅓ of ion range
    0.15 mm to several mm
  Maximum extension of 50 mm in beam direction including slice thickness and cooling fins to meet optics requirements
  5000 rpm and 30 cm diameter to limit maximum temperature and amplitude of temperature changes
Multi-slice target / heat exchanger
Shield block
Radiation resistance and vacuum compatible motor

## Slide 5: FRIB Production Target Challenges
Thermo-mechanical challenges
  High power density: ~ 20 - 60 MW/cm³
    High temperature: ~ 1900 ºC: Evaporation of graphite, stress
  Rotating target
    Temperature variation: Fatigue, Stress waves through target
Swift Heavy Ion (SHI) effects on graphite
  Radiation damage induce material changes
    Property changes: thermal conductivity, tensile and flexural strength, electrical resistivity, microstructure and dimensional changes, …
  Swift heavy ions (SHI) damage not well-known
  5·1013 U ions/s at 203 MeV/u may limit target lifetime
    Fluence of ~9.4·1018 ions/cm² and 10 dpa estimated for 2 weeks of operation
Similar challenges at
  Facility for Antiproton and Ion Research (FAIR) at GSI
  Radioactive Ion Beam Factory (RIBF) at RIKEN

## Slide 6: Irradiation Test at UNILAC at GSI/Darmstadt
Polycrystalline isotropic graphite
  2 Grades MERSEN 2360 (5 μm ) / 2320 (13 μm)
Irradiation test at UNILAC at GSI/Darmstadt
  Au-beam 8.6 MeV/u
    Up to 5.6·1010 ions/cm²·s and fluence up to 1015 ions/cm²
      Equivalent to a fluence of 1018 ions/cm² for FRIB beam energy or 2 days of operation
    Electronic energy loss ≈ 20 keV/nm
  Ohmic heating (up to 35 A, 250 W) of samples to different temperature during irradiation
I = 35 A
I = 35 A + beam
Tmax = 1480 (± 30 ºC)
Tmax = 1635ºC

## Slide 7: Radiation Damage Studies in Graphite [1] Annealing of Damage at High Temperature (> 1300ºC)
Swelling is completely recovered at 1900ºC
X-Ray Diffraction analyses
TEM analyses
1 A - 350C 1014 cm-²
11 A - 750°C 1014 cm-²
25 A - 1205°C 1014 cm-²
35 A - 1635°C 1015 cm-²

## Slide 8: Radiation Damage Studies in Graphite [2] Annealing of Damage at High Temperature (> 1300ºC)
Annealing at high temperature confirmed
Young’s Modulus of irradiated graphite samples - 197 Au fluence 1014 ions/cm²
Thermal conductivity change of irradiated graphite samples - 197 Au fluence 1014 ions/cm²
Electrical resistance change of irradiated graphite samples - 197 Au
pristine
pristine

## Slide 9: NSCL-FRIB Strippers Challenges
It is known that thin foils (stripper) used in accelerator suffer a quick degradation due to radiation damage such as swelling and thermo-mechanical changes
  Limits the lifetime of few hours
How can we improve the lifetime?
  Annealing at high temperature
  Influence of nano-structure on annealing
  FRIB full intensity Li film stripper
  ….

## Slide 10: NSCL-FRIB Strippers Radiation Damage
Recent tests at NSCL have shown quick deterioration of graphite foils under heavy ion bombardment due to thermal and mechanical stresses and radiation damage
  Carbon irradiated with Pb beam @ 8.1 MeV/u
    Se= 24 keV/nm, fluence = 4.5·1016 ions/cm²
F. Marti et al., "A carbon foil stripper for FRIB", TUP 106, Proceedings of Linear Accelerator Conference LINAC2010, Tsukuba, Japan, TUP105, 2010.
SEM photographs of unused carbon foil (left) showing a small pinhole for illustration and a foil exposed to 8.1 MeV/u Pb beam

## Slide 11: NSCL-FRIB Strippers Irradiated Strippers at NSCL
Current carbon strippers used at NSCL

## Slide 12: Improvement of the lifetime
Previous studies [3] showed annealing effects of radiation damage at high temperature. The heating by the beam was evaluated to produce temperatures of up ~900 ºC. A clear tendency of increased lifetime with irradiation temperature was observed.
The lifetime of the 10 multilayer foil C-DLC-B was significantly higher (factor 3) than the standard C-NSCL foils. The 10 multilayer foil C-DLC was somewhat superior (about a factor 2) as compared to the standard foils.
Lifetime time (μA·h/cm²) as a function of the irradiation temperature and the microstructure of graphite stripper foils.
[3] S. Fernandes et al., “In-Situ Electric Resistance Measurements and Annealing Effects of Graphite Exposed to Swift Heavy Ions”, Nucl. Instrum. Methods Phys. Res. B 314 (2013) 125-129.

## Slide 13: Summary and Conclusions
Heavy-ion irradiation tests and annealing studies performed in the context of high-power target and strippers for high intensity accelerator were performed
High temperature annealing of heavy-ion induced radiation damage observed in production target
  First experiment of this kind
  Confirmed by several analysis
Graphite as a material for FRIB beam production targets promises sufficient lifetime
High temperature annealing of heavy-ion induced radiation damage observed in NSCL strippers

## Slide 14: Acknowledgements
FRIB/NSCL Michigan State University
  Mikhail Avilov, Saul Beceiro Novo, Sandrina Fernandes, Felix Marti, Mike Schein, Andreas Stolz, Genevieve West
GSI Helmholtzzentrum für Schwerionenforschung GmbH
  Markus Bender, Markus Krause, Daniel Severin, Marilena Tomut, Christina Trautmann
University of Michigan
  Rodney Ewing, Maik Lang, Weixing Li

## Slide 15
Thank you for your attention
FRIB construction area – October 27 2014

## Slide 16: NSCL-FRIB Strippers Lifetime measurement at NSCL
Effect of the temperature on lifetime improvement observed at NSCL
Preliminary results
78 Kr14+ @ 13 MeV/u
20 Ne @ 3.2 MeV
Sugai et al., NIMB 269 (2011) 223-228