## Slide 1: Graphite progress update
BJ Marsden and G Hall
Nuclear Graphite Research Group, School of MACE, The University of Manchester
28 March 2013

## Slide 2: Introduction
POCO vs. “nuclear grade” graphite
  HOPG as an example
Environment = LBNE
  1 dpa
  ≤300ºC
  non-oxidising environment
Neutron c.f. proton irradiation
Continuous c.f. pulsed irradiation
Some recommendations

## Slide 3: POCO vs. “nuclear grade” graphite
POCO chosen based upon
  past experience (irradiation stability)
  grain structure (isotropy)
  high strength
Similar (historical) conclusions in fission area
  used as specimen holders, restraints etc.
  manufacturing limits  restricted usage
POCO different than nuclear grades
  ultrafine grain size (1-5 µm c.f. ≥10 µm)
  fine pore structure (0.3-0.8 µm c.f. ≥8 µm)
  CTE near perfect (~8 × 10-6 K-1 c.f. ~4 × 10-6 K-1)

## Slide 4: POCO vs. “nuclear grade” graphite
POCO is probably a sintered material
  previous differences
  no visible “binder” phase
  often no impregnation
POCO can have a lower graphitisation temperature than standard (2800ºC) e.g.
  AXF-Q1 = 2300ºC
  ZXF-5Q = 2500ºC
  AXF-8Q1 = 2800ºC
  affects properties and irradiation behaviour
POCO AXF-8Q1
EGCR (nuclear grade)
Replica electron micrographs (Pitner, 1971)
Notes: First letter possibly particle size (Z = 1 µm, A = 5 µm)
Third letter possibly amount of porosity (F = 20%, Z = 28%)
Don’t know what last number relates to.

## Slide 5
Grade | ZXF-5Q | AXF-8Q1 | AXZ-5Q | Gilsocarbon | IG-430 | IG-110
Comment | candidate | historical experience (fission) | historical experience (fission) | historical experience (fission) | historical experience (fission) & similar to IG-43 | historical experience (fission)
Particle size (µm) | 1 | 5 | 5 | 500 | 10 | 20
Pore size (µm) | 0.3 | (0.3) | 0.7 | 42 | - | 16
Density (g/cm3) | 1.78 | 1.80 | 1.66 | 1.81 | 1.82 | 1.77
Total porosity (% volume) | 20 | (20) | 28 | 20 | 19 | 21
Open porosity (% of total) | 80 | (80) | 90 | 55 | 65 | 58
Graphitisation temperature (ºC) | 2500 | 2800 | 2500 | ≥2800 | ≥2800 | ≥2800
Notes: The 0 in IG-430 means it has been purified.

## Slide 6: Dimensional change
400 to 700ºC
  data on POCO grades
  negligible dimensional changes
  little data
  nuclear grades shrink within this range
≤300ºC
  no data on POCO grades
  expect dimensional changes to be greater
    possibly significant
  lower temperature = greater the rate of change
AXF-8Q1
AXZ-5Q1
Dimensional changes (Pitner, 1971)
~1 dpa
~1 dpa

## Slide 7: Dimensional change
against grain (AG)
Dimensional changes of Pile Grade A (PGA) graphite
with grain (WG)
~1 dpa
~1 dpa
decreasing temperature
decreasing temperature

## Slide 8: Dimensional change
Decrease in graphitisation temperature = increase in dimensional change rate
  at 1 dpa difference between 2500ºC and 2800ºC is likely to be negligible
PGA graphitised to various temperatures and irradiated at 600ºC (Brocklehurst and Kelly, 1993)

## Slide 9: Dimensional change
Dimensional change under load
  dimensional changes different due to irradiation creep
    reduces stresses in graphite components
  target under initial compressive load
    shrinkage increases when already shrinking (≥300ºC)
    assume expansion decreases when already expanding (<300ºC)
  complex interaction in target
    fluence distribution
    temperature distribution
    boundary conditions
Target for LBNE

## Slide 10: Dimensional change
Recommendations
  keep graphite at higher temperatures (~300ºC)
  graphitisation at 2500ºC should be ok
  conduct stress analysis of target
    realistic fluence and temperature distributions
Additional recommendation
  conduct experiments on POCO at temperatures of interest

## Slide 11: Helium production
Usually not considered in fission
  negligible helium production
  exception when graphite was doped with 10B
When helium production is not negligible
  highly oriented pyrolytic graphite (HOPG) experiences increased dimensional changes and exfoliation/delamination/flaking of layers
    helium trapped in cavities
HOPG doped with 10B and irradiated 650ºC (Kelly and Mayer, 1969)

## Slide 12: Helium production
When helium production is not negligible
  POCO and nuclear grade graphites have significant amounts of open porosity
    some helium can escape
    remainder could influence dimensional changes
      helium effect secondary to effect of boron on nucleation of interstitial loops
Recommendation
  conduct further investigations and/or scoping calculations to determine relevance
Dimensional changes of boronised graphite irradiated to 0.13 dpa at 300ºC (Maruyama and Harayama, 1992)

## Slide 13: Thermal conductivity
Rapid reduction in thermal conductivity with fluence
  rate of decrease increases with decreasing temperature
Thermal conductivity of various irradiated graphites (Moore et al., 1973)
~1 dpa
~1 dpa
Thermal conductivity of PGA irradiated at various temperatures (Birch and Brocklehurst, 1987)
decreasing temperature