## Slide 1: Graphite progress update
BJ Marsden and G Hall
Nuclear Graphite Research Group, School of MACE, The University of Manchester
22 July 2013

## Slide 2: Thermal shock
Graphite has good thermal shock resistance (R)
  use as crucibles, moulds, dies, and electrodes
Unirradiated (calculated)
  POCO ZXF-5Q ≈ 47 kW/m
  Toyo Tanso IG-430 ≈ 112 kW/m
Reduces with irradiation
Reduces with oxidation
Notes: ZXF-5Q average due to low thermal conductivity, high Young’s modulus, and high CTE. None of POCO grades examined have an above average resistance.
IG-430 good due to high thermal conductivity, lower CTE, and lower Young’s modulus.
Limited experimental data

## Slide 3: Thermal shock
R (kW/m)
Thermal shock resistance of graphites before and after irradiation to 11-15 × 1020 n/cm2 (>0.18 MeV) at 750-1000ºC (Sato et al., 1989)
Thermal shock resistance of graphites before and after irradiation to 16-17 × 1020 n/cm2 (>0.18 MeV) at 600-850ºC (Sato et al., 1980)
Weight loss (%)
ln(R/R0)
Thermal shock resistance of oxidised IG-430 graphite (Kurumada et al., 1997)

## Slide 4: Summary
LBNE
  POCO ZXF-5Q, 1 dpa, ≤300ºC, no oxidation
T2K
  Toyo Tanso IG-430, 1 dpa, 700 to 800ºC, ~8% oxidation
No ‘show stoppers’ found
  no obvious better choice of grade
  recommend (scoping) thermo-mechanical analyses
    irradiation-induced dimensional and materials properties changes
    oxidation
  recommend further calculations (or experiments) on thermal shock resistance
Notes: POCO good choice for LBNE as reduced dimensional changes useful as running at lower temperatures.
However, thermal shock resistance not particularly high
IG-430 good choice for T2K as should have a higher thermal shock resistance and POCO experience DCs at these temperatures.