## Slide 1: PSI experience with High Power Target Design and operational considerations for muon production [with slides from Th.Prokscha, G.Heidenreich]
Mike Seidel
Paul Scherrer Institut
April 19, 2013,
Brookhaven National Laboratory

## Slide 2: Outline
overview PSI targets and parameters
thermomechanical target aspects, mechanics and supporting infrastructure
example for μ-beam capture and transport
discussion

## Slide 3
50 MHz proton cyclotron, 2.2 mA, 590 MeV, 1.3 MW beam power (2.4 mA, 1.4 MW test operation)
PSI proton accelerator complex
UCN
Comet cyclotron (superconducting), 250 MeV, 500 nA, 72.8 MHz
LEM
GPD
High field (9.5T) mSR
GPS/LTF
Dolly
SINQ, neutron spallation source
proton therapy, irradiation facility
MEG

## Slide 4: Meson production targets used at PSI
Target M Target E
1974-80 < 100 mA Be, Graphite *) Be, Graphite *)
 190 mm  190 mm
0.9 g/cm2 22 g/cm2
Pyrolitic graphite**)
22 g/cm2
1980-89 250 mA Graphite *) Graphite *)
 320 mm  280 mm
0.9 g/cm2 18 g/cm2
since 1990 0.5 - 2 mA Graphite *) Graphite *)
 320 mm  450 mm
0.9 g/cm2 10 g/cm2 (60 mm)
or 7 g/cm2 (40 mm)
*) rotating wheel target **) static target

## Slide 5: Target-M design
P-BEAM
Target M:
Mean diameter: 320 mm
Target thickness: 5.2 mm
Target width: 20 mm
Graphite density: 1.8 g/cm3
Beam loss: 1.6 %
Power deposition: 2.4 kW/mA
Operating Temperature: 1100 K
Irradiation damage rate:0.12 dpa/Ah
Rotational Speed: 1 Turn/s

## Slide 6: Exchange of Target-M
Operation of the remotely controlled shielded flask
Dose rate ~10 mSv/h

## Slide 7: Design of the proton channel between target-E and the beam dump
BEAM DUMP

## Slide 8: Working platform / Operation of the remotely controlled shielded flask

## Slide 9: Design of Target station E
p
TARGET E: 6/4cm
Beam losses: 18/12 %
COLLIMATOR 2 & 3
Beam losses: 22/18 %
INFLATABLE ALL-METAL SEAL
TARGET CHAMBER
BACKWARD SHIELDING
FORWARD SHIELDING
SHIELDING COLLIMATOR

## Slide 10: Target-E design
p-beam
Drive shaft
BALL BEARINGS *)
Silicon nitride balls
Rings and cage silver coated
Lifetime 2 y
*) GMN, Nürnberg, Germany
SPOKES
To enable the thermal expansion of the target cone
TARGET CONE
Mean diameter: 450 mm
Graphite density: 1.8 g/cm3
Operating Temperature: 1700 K
Irradiation damage rate: 0.1 dpa/Ah
Rotational Speed: 1 Turn/s
Target thickness: 60 / 40 mm
10 / 7 g/cm2
Beam loss: 18 / 12 %
Power deposition: 30 / 20 kW/mA

## Slide 11: Drive motor & permanent-magnet clutch
Record of the drive torque for the rotation
DC-motor
Permanent-magnet clutch
Ball bearing
vacuum
air pressure

## Slide 12: design of graphite wheel
The gaps allow unconstrained dimensional changes of the irradiated part of the graphite.

## Slide 13: Temperature & stress distribution (2mA, 40 kW)
1700 K
600 K
5 MPa

## Slide 14: Maintenance of the target-insert in the hot-cell
Exchange parts:
horizontal drive shaft

## Slide 15: Operational limits of the rotating graphite & beryllium cones for target-E
Temperature (K)
Safety factor syp/s
Evaporation rate (mg/g/year)
Be
C
I(mA): Proton current
D(m) : Mean target diameter
e* : effective emissivity
3mA operation of Target-E
D = 0.45 m
e* = 0.7
[G.Heidenreich]

## Slide 16: Lifetime of the pyrolitic graphite targets due to irradiation-induced dimensional changes
Operational parameters:
Proton current: 100 A
Peak current density: 1000 A/cm2
Peak temperature: 1800 K
Lifetime limits:
Proton fluence: 1022 p/cm2
Integrated beam current: 50 mAh
Irradiation-induced swelling: ~ 10 %
Irradiation damage rate: ~ 1 dpa
p
Swelling of the target after irradiation
1022 p/cm2
p
-30
-20
-10
0
10
20
30
40
50
60
70
0
2
4
6
8
10
12
Dimensional change (%)
——
1273 - 1423 K
——
1473 - 1573 K
Neutron Fluence
J. Bokros et. al, Carbon 1971,Vol. 9,p. 349
* 1021 N/cm2
~ 1 dpa

## Slide 17
Muon- capture:
Layout of the mE4 high-intensity m beam [Th:Prokscha]

## Slide 18
p/p (FWHM): 5% - 9.5%
TRANSPORT: PSI Graphic Transport
framework by U. Rohrer, based on a
CERN-SLAC-FermiLab version by
K.L. Brown et al.
x
y
y
x
3% p/p 1st
0% p/p 1st
3% p/p 2nd
TRACK: Three-dimensional Ray
Tracing Analysis Computational
Kit, developed by PSI magnet
section (V. Vrankovic, D. George)
Transport and TRACK calculations

## Slide 19
Solenoid versus quadrupole
➨
➨
Mixing of phase space might lead to an increase of beam spot size
Focusing powers PS,T of solenoid and triplet at same power dissipation in device:
Rotation  of phase space:
90x-y PS exchanged
Azimuthal symmetry of solenoids leads to larger acceptance
First order transfer matrix for static magnetic system with midplane symmetry:
First order transfer matrix for a solenoid, mixing of horizontal and vertical phase space:

## Slide 20
Bmax = 3.5 kG
Øi = 500 mm
Double-solenoid WSX61/62

## Slide 21
Installation of a section of mE4 in 2004

## Slide 22
Discussion
PSI concept is optimized for dual use of beam (Meson and Neutron Production); C = low-z material; strong focus at target: minimize emittance growth
beam loss at 40mm C-target:
  10% inelastic nuclear interactions; 20% collimation of spent beam
rotating graphite target concept with radiation cooling was optimized over many years; lifetime limited by anisotropy of graphite and resulting wobbling from radiation damage; pyrolithic graphite not suited!
service and exchange systems, Hotcell are VERY IMPORTANT for practical operation
Muon figures: ≈5∙108 μ+/s possible @p=28MeV/c; p/p=9.5%FWHM;
x/y = 5/10∙10-3m∙rad
T. Prokscha, et al., Nucl. Instr. and Meth. A (2008), doi:10.1016
/j.nima.2008.07.081
activation after one year: order of 1…5 Sv/h; thanks to Graphite this is low compared to heavy target materials!
issues: Tritium production in porous material; oxidation of graphite with poor vacuum of 10-4mbar; carbon sublimation at higher temperatures; wobbling of wheel caused by inhomogeneous radiation damage