## Slide 1
Tests Using
The “Little Wire Test” Equipment
(Apr. 4, 2013)
J. R. J. Bennett1, G. Skoro1(2), P. Loveridge1, A. Ahmad2
Fatigue Life of Tungsten at High Temperatures and High Strain Rates.
Fatigue Life of Tungsten at High Temperatures and Low Strain Rates (quasi-static).
Emissivity of Tungsten and Surface Roughness
Oxidation of Tungsten at High Temperatures
1 Rutherford Appleton Laboratory, Chilton, Didcot, Oxon, OX11 0QX
2 Department of Physics and Astronomy, Sheffield University, Sheffield, S3 7RH

## Slide 2
springs
outer conductor
ceramic insulator
chuck
test wire
graphite jaws
cap
inner conductor
to
pulsed
power
supply
fixed end
free end
viewing apertures
laser Doppler vibrometer
  Schematic diagram of “The Little Wire”

## Slide 3
  “The Little Wire” Equipment

## Slide 4
Vacuum chamber
LDV
Coaxial cables (current from power supply)
LDV = Laser Doppler Vibrometer

## Slide 5: Operating Principle
Magnitude and frequency of wire oscillations measured using LDV
  Characteristic frequency gives a direct measure of the material Elastic Modulus
  Induced dynamic stress is calculated via LS-DYNA simulation and verified by cross-comparison with measured surface velocities
G.P. Skoro et al. / Journal of Nuclear Materials 409 (2011) 40-46

## Slide 6: Why High Strain-Rate Measurements?
The main issue for beam-facing materials used in target systems (targets, beam windows, beam dumps, containment vessels, etc.) is the magnitude and the rate of change of deposited energy density (J/cc).
In a regime where beam pulse length is short compared to characteristic expansion times and thermal conduction timescales we can make the following simplifications: ΔT≈Eden/ρ.Cp Thermal Stress ≈ α.E.ΔT
With increasing beam power, and decreasing pulse length, the estimate of material strength and corresponding lifetime based on simple, quasi-static equations is no longer accurate.
In these cases the materials respond dynamically and they behave differently than under quasi-static loading. In order to address this problem the fundamental material properties and corresponding strength have to be measured under dynamic conditions.

## Slide 7: Dynamic Young’s Modulus of Tungsten
G.P. Skoro et al. / Journal of Nuclear Materials 409 (2011) 40-46

## Slide 8: Yield Strength Measurements
J.R.J. Bennett et al., Nucl. Instr. And Meth. A (2011), doi:10.1016/j.nima.2011.03.036

## Slide 9
Strain rates shown in s-1.
Strength of Tungsten versus Temperature
and
Lifetime,
in Millions of Pulses
Lifetime Evaluation (Cycles to failure)

## Slide 10: Why Low Strain-Rate Measurements?
In some target applications the rate of change of stress and Strain are ‘low’. i.e. we have a ‘quasi-static’ state of stress:
e.g. Proposed Mu2e Target:
Unusually long (~50 msec) beam spills give rise to quasi-static cycles
e.g. ISIS target Cladding:
Stresses rise and fall between pulses on the timescale of thermal conduction

## Slide 11: Low Strain Rate Tests in the Little-Wire Test Rig
Operating Principle:
Use resistive (Joule) heating from an electric current pulse to preferentially heat the centre of a disk
Pulse length long enough to give ‘static’ stress field (do not want inertial stresses)
Inter pulse gap long enough for transient stress component to decay (on the timescale of thermal conduction)
Rep rate of 10’s of Hz (to allow accelerated testing of target lifetime cycles)

## Slide 12: Sample Geometry Concept
Example: Mu2e Target Test
  Machine features into a 6mm diameter 160mm long tungsten bar i.e. this is a ‘full size’ test
  Means we can test the stock material / surface treatment that we intend to use for the real target!
D.C. Current Distribution
160A D.C - equivalent heating to 1.6kA 1msec pulses @20 Hz
Volumetric Joule heating (J2ρ) mostly occurs over this length
Steady-State Von-Mises Stress Field
Tension
Compression
Steady-State Temperature
Qrad ~ 200W

## Slide 13: Tuneable Temperature and Stress Cycles
Can tune the sample geometry to achieve representative temperature and stress cycles for a given application
Can fine tune the stress cycle and operating temperature online by varying the peak current and rep rate.
Example: Temperature and stress cycles in the proposed Mu2e test specimen (1.6 kA, 1 msec half sine-wave current pulses @ 25Hz)
Tuned to match the target operating conditions

## Slide 14: First Tests Using Tantalum Foil
‘2D version’ of the proposed Mu2e test piece
25 μm tantalum foil
1×10-5 mbar vacuum
DC Current = 6.0 A
1120 ⁰C
960 ⁰C
Temperature Measurements
Specimen Dimensions (mm)
Experimental Setup

## Slide 15: Thermal Emissivity and Surface Roughness
The surface roughness alters the emissivity. Measure the emissivity and roughen the surface - with abrasives – cut groves in the surface – etc.
Look with optical pyrometer, Compare outer surface to tube interior (~black body)
Tungsten tube with a small hole drilled in one side. (rolled sheet or machine from solid)
D.C. current
Place thermocouple inside for cross-check (optional)
Use an Optical Pyrometer to:
  Measure black body temperature by looking through the hole – Tbb
  Measure surface temperature – Ts
ε = Ts/Tbb

## Slide 16: Oxidation
Tungsten must be in an inert atmosphere or vacuum to avoid chemical oxidation when hot.
We need to know the maximum vacuum pressure at which the hot tungsten will have a long life.
There are measurements in the literature, - but if they are insufficient we will make our own in the measurements in the “little wire test equipment”.
oxygen, air or water
Hot wire or foil
Pressure gauge
To high vacuum pump
QMA
Schematic diagram of the system
Leak valve

## Slide 17
Summary of the “Little Wire Test” Equipment
The equipment is ideally suited to measuring the ultimate strength of materials at very high temperatures at all strain rates.
It has been used to determine the properties of tungsten at high strain-rate :
Lifetime (cycles to failure) as a function of stress and temperature.
Strength as a function of temperature.
Young’s modulus of elasticity as a function of temperature.
It is easily adaptable to a variety of other measurements:
Lifetime evaluation at low strain-rate
Emissivity measurements
Oxidation Lifetime studies